# Do the generalized thermoelasticity theories differ for porous GPL-reinforced cylinders? A four-theory comparison under ramp and impulsive thermal loading

Authors. [Author 1]ᵃ, [Supervisor 1]ᵃ, [Supervisor 2]ᵃ ᵃ Department of Mechanical Engineering, Persian Gulf University, Bushehr, Iran

Author order to be settled with the supervisors. Add the thesis-derivation footnote. Cite Paper 1 (formulation and validation) as submitted / in press.

Target journal. Journal of Thermal Stresses (alternates: Acta Mechanica, Continuum Mechanics and Thermodynamics)

## Abstract

Four thermoelasticity theories — classical coupled Fourier, Lord–Shulman, dual-phase-lag and Green–Naghdi type III — are in routine simultaneous use, and a designer choosing among them has little quantitative guidance on when the choice actually changes the answer. This paper supplies that guidance for a structural class in which it has not been examined: a multilayer porous graphene-platelet-reinforced thick-walled cylinder, whose effective properties vary by an order of magnitude through the wall. The four theories are solved on an identical layerwise differential quadrature discretization with matched parameters, under two loadings chosen to bracket practice — a smooth internal temperature ramp and a short Gaussian pulse. Under the ramp at a mild relaxation time the three dissipative theories are nearly indistinguishable, peaking at 0.950 (Fourier), 0.956 (dual-phase-lag) and 0.962 (Lord–Shulman); the dual-phase-lag result interpolates between the other two exactly as its structure predicts, and reduces identically to Fourier when the two lags are equal. Green–Naghdi type III behaves qualitatively differently: it overshoots early and strongly to 1.581 and is still at 0.870 at the end of the observation window, because its energy equation carries no mechanism to dissipate the thermal wave. Replacing the ramp with an impulsive pulse separates Fourier from Lord–Shulman decisively: the classical pulse arrives early, smeared and weak (0.195), and has effectively vanished by the end of the window, whereas the Lord–Shulman pulse arrives later, two and a half times stronger (0.478), and persists as a coherent wave packet. A relaxation-time sweep shows the mid-wall overshoot growing monotonically from 0.953 to 1.271, and the measured wave arrival matching the hyperbolic prediction. The practical conclusion is loading-dependent: for slow thermal loading the classical theory is defensible for this material class, while for impulsive loading it substantially under-predicts the severity of the event.

Keywords. Generalized thermoelasticity; Lord–Shulman; dual-phase-lag; Green–Naghdi; second sound; graphene platelets; functionally graded porosity

## 1. Introduction

[Target ≈ 1000 words.]

Paragraph 1 — the paradox and its repairs. Fourier’s law makes the heat equation parabolic, implying that a disturbance anywhere is felt instantly everywhere. The Cattaneo–Vernotte modification introduces a flux relaxation time and restores a finite propagation speed; Lord and Shulman built the first thermodynamically consistent generalized thermoelasticity on it. Introduce second sound.

Paragraph 2 — the family of theories. Lord–Shulman (one relaxation time); Green–Lindsay (two); Green–Naghdi types I, II and III, with type II famously dissipationless and type III containing both a conductivity and a thermal-displacement conductivity; Tzou’s dual-phase-lag with separate flux and gradient lags. Note the known result that dual-phase-lag collapses onto Fourier when the two lags are equal — useful later as an internal consistency check.

Paragraph 3 — where they have been compared. Comparative studies exist, largely for homogeneous media or simple functionally graded profiles, and largely under idealized shock loading. State clearly what is missing: a comparison on a strongly heterogeneous structure, where the through-thickness variation of conductivity, stiffness and thermal inertia is itself large, and under more than one loading type, so that the loading-dependence of the answer can be seen.

Paragraph 4 — why this material class is the interesting test. In a porous GPL-reinforced wall the effective conductivity varies by an order of magnitude across the thickness because of the percolation behaviour of the graphene network, and the porosity independently modulates the thermal inertia. A thermal wave crossing such a wall is refracted, partially reflected at every property change, and damped unevenly — precisely the conditions under which theories that differ only in their wave term might be expected to diverge most.

Paragraph 5 — contribution.

- A four-theory comparison (Fourier / Lord–Shulman / dual-phase-lag / Green–Naghdi III) on an identical discretization with matched parameters, for a multilayer porous GPL-reinforced cylinder.

- The comparison repeated under two loading types, establishing that the answer to “does the theory matter?” is loading-dependent, not material-dependent alone.

- Quantification of the Green–Naghdi III departure and attribution of it to the absent dissipation mechanism.

- A relaxation-time sweep verifying that the measured wave arrival obeys the hyperbolic prediction, with the coupled-field damping of the wave quantified separately.

## 2. The four theories in a common form

Write all four energy equations in a single parameterized form so that the comparison is manifestly like-for-like. With θ=T−Tref and e the dilatation:

Classical coupled (Fourier).

ρc θ+βT0 e=k∇2θ

Lord–Shulman. Flux relaxation τ0 applied to both the storage and the coupling term:

ρc (θ+τ0θ)+βT0(e+τ0e)=k∇2θ

Dual-phase-lag. Flux lag τq and gradient lag τT:

ρc (θ+τqθ)+βT0(e+τqe)=k∇2θ+kτT∇2θ

Setting τT=τq recovers Fourier; setting τT=0 recovers Lord–Shulman.

Green–Naghdi type III. With the thermal-displacement conductivity k*:

ρc θ+βT0 e=k*∇2θ+k∇2θ

[State the matched-parameter choices explicitly: τq=τ0 and τT=τq/2 for DPL, and k*=k/τ0 for GN-III so that its wave speed equals the Lord–Shulman one. Matching the wave speeds is what makes the GN-III difference attributable to the dissipation structure rather than to a different propagation speed. Note the documented approximation that the flux boundary condition is kept in standard form for GN-III.]

[Figure 1: theory taxonomy schematic — figures_ch123/theory_taxonomy.png.]

## 3. Model, discretization and verification — summary

Keep this section deliberately short and cite Paper 1 for the full treatment.

Axisymmetric multilayer porous GPL-reinforced hollow cylinder; Halpin–Tsai effective modulus, rule-of-mixtures density and specific heat, percolation-type effective conductivity, porosity applied pointwise. Layerwise differential quadrature with Chebyshev grids in (r,z); Newmark time integration with δ=1/2, β=1/4; row equilibration before a single factorization.

Verification is reported in full in Paper 1. The test that matters here is the quantitative second-sound benchmark: an exact Fourier–Bessel eigenfunction reference, itself verified to 1.9 × 10⁻¹⁶ of ΔT in the steady limit, to 4 × 10⁻⁶ for hyperbolic causality ahead of the front, and to 0.16 % against the analytic ray law for the front-jump ratios. The present solver matches it to 0.32 % pointwise and 0.065 % in L₂, with monotone convergence under refinement. This establishes that the wave features discussed below are resolved physics and not discretization artefacts — an essential precondition for a paper whose subject is the wave term.

Reference case. Ri=1.0 m, Ro=1.5 m, L=2.1 m, NL=7; uniform graphene at 0.3 % and uniform porosity; inner surface ramped 300 → 600 K with t0=2 s; internal pressure 50 MPa; outer convection hc=10 W/m²K to 300 K; simply supported ends; Nr=15, Nz=11, Δt=1 s to 3000 s. Dimensionless quantities as in Paper 1, with the wall thickness as length scale and α=8.97×10−5 m²/s.

## 4. Results

### 4.1 The relaxation time and the wave signature

Before comparing theories it is necessary to establish that the Lord–Shulman wave is real and correctly placed. The dimensionless relaxation time is swept over τ*=0.04, 0.15, 0.44, 0.87 against the Fourier limit. The peak mid-wall temperature rises monotonically:

| case | τ*​ | peak T* | Fo at peak |
| --- | --- | --- | --- |
| Fourier | 0 | 0.950 | 2.153 |
| LS | 0.04 | 0.953 | 2.153 |
| LS | 0.15 | 0.962 | 1.373 |
| LS | 0.44 | 1.166 | 1.675 |
| LS | 0.87 | 1.271 | 2.141 |

Two features are worth noting. The peak exceeds unity from τ*=0.44 upward — that is, the mid-wall temperature exceeds the inner-surface boundary value, which is impossible under Fourier conduction and is the superposition of the incident and reflected thermal waves. And the peak arrives earlier as the relaxation time grows into the intermediate range, because the transport mechanism shifts from diffusion to propagation.

The wave speed of the reference material, v=α/τ0, predicts a full-wall crossing at Fo=τ*; the observed first arrival matches this, which is the quantitative confirmation that what is seen is the second-sound front and not a numerical transient.

[Figure 2: figures_ch4_color/C_relaxation.png, or the finer-mesh C_relaxation_N35 variant. Figures 3–4: wave-front snapshots BASE_wavefront.png, C_TAU_087_wavefront.png.]

A note on the magnitude of τ0. The relaxation times that make the wave clearly visible here are far above any measured value for a polymer-matrix composite. They are used as a parametric device to expose the structure of the solution, not as a claim about the material — and this should be stated plainly in the paper rather than left for a referee to raise. The physically realistic regime for this material is the small-τ* end, where the paper’s own conclusion is that the theory choice barely matters under slow loading.

### 4.2 The four theories under ramp loading

With matched parameters the peak mid-wall temperatures order as

Fourier 0.950 < DPL 0.956 < Lord–Shulman 0.962 ≪ Green–Naghdi III 1.581

Two observations follow.

The three dissipative theories nearly coincide. At the mild reference relaxation time the spread between Fourier and Lord–Shulman is about 1.3 %, and the dual-phase-lag result sits between them, as the structure of its energy equation requires. As an internal check, setting τT=τq reproduces the Fourier solution to nine digits — the known collapse, recovered here as a verification of the implementation rather than as a new result.

Green–Naghdi III stands apart, and qualitatively so. Its peak of 1.581 arrives early, at Fo≈0.33, and the field then relaxes only slowly, still at 0.870 at the end of the window where the other three have settled. The cause is structural: the GN-III energy equation, with the wave speed matched to Lord–Shulman’s, lacks the dissipative term that damps the propagating disturbance in the other theories, so the energy injected at the inner surface continues to slosh through the wall instead of decaying. The difference is therefore not a matter of degree that could be absorbed by re-tuning a parameter — it is a difference in long-time character, and it means a GN-III model of this structure will predict persistent thermal cycling that the other three theories do not.

[Figure 5: figures_ch4_color/T3_theories.png.]

### 4.3 Impulsive loading separates the theories

The ramp is replaced by a short Gaussian pulse of the inner-surface temperature, and the Fourier and Lord–Shulman responses are compared at mid-thickness:

| theory | peak T* | Fo at peak | T* at end of window |
| --- | --- | --- | --- |
| Fourier | 0.195 | 0.176 | 0.019 |
| Lord–Shulman | 0.478 | 0.306 | 0.001 |

Under Fourier conduction the pulse reaches mid-thickness early, smeared and weak, and has practically disappeared by the end of the interval — the signature of diffusion, which spreads a disturbance in time as it transports it. Under Lord–Shulman the pulse arrives later, because it travels at a finite speed, roughly two and a half times stronger, because it travels as a coherent packet rather than spreading, and leaves persistent oscillations behind it as the packet reflects within the wall. A sharp second-sound front is visible marching through the thickness.

This is the paper’s most practically consequential result. For impulsive thermal loading the classical theory does not merely shift the timing — it under-predicts the peak transient temperature at mid-wall by a factor of about 2.5, and therefore under-predicts the associated transient thermal stress. A design screened with a Fourier model against an impulsive event is non-conservative.

[Figure 6: figures_ch4_color/M_gauss_shock.png.]

### 4.4 Thermoelastic damping of the wave

Comparing the fully coupled model with the uncoupled one (dilatation-rate term removed from the energy equation) isolates the mechanical feedback on the thermal field. The uncoupled model overestimates the peak mid-point temperature by about 1.2 % (0.937 against 0.926) at the reference conditions, with the largest discrepancy occurring exactly at the wave fronts. Part of the thermal energy is continuously converted into mechanical work — a thermoelastic damping of the thermal wave — so the uncoupled model is non-conservative where the wave is sharpest. The effect is modest at the mild reference relaxation time but grows with the strength of the wave, which means that the loading regime where the generalized theory matters most is also the regime where dropping the coupling is least acceptable.

[Figure 7: figures_ch4_color/I_coupling.png.]

## 5. Conclusions

- For a multilayer porous GPL-reinforced cylinder under slow thermal loading at a physically plausible relaxation time, the classical Fourier, dual-phase-lag and Lord–Shulman theories give nearly the same answer (0.950, 0.956, 0.962). The choice between them is not the leading source of uncertainty.

- Under impulsive loading the same theories diverge decisively: the Lord–Shulman pulse reaches mid-wall about 2.5 times stronger than the Fourier one and persists, while the classical pulse smears and vanishes. The answer to “does the theory matter?” is therefore a property of the loading, not of the material alone.

- Green–Naghdi type III is qualitatively different from the other three even at matched wave speed, overshooting to 1.581 and relaxing only slowly, because its energy equation has no dissipative mechanism. It should not be treated as interchangeable with Lord–Shulman.

- Dual-phase-lag interpolates between Fourier and Lord–Shulman and collapses onto Fourier at equal lags, recovered here to nine digits as an implementation check.

- Full field coupling damps the thermal wave; the uncoupled approximation is non-conservative at the wave fronts, and increasingly so as the wave strengthens.

## References

[Minimum set; renumber to journal style.]

- Lord HW, Shulman Y. A generalized dynamical theory of thermoelasticity. J Mech Phys Solids 1967;15(5):299–309.

- Green AE, Naghdi PM. Thermoelasticity without energy dissipation. J Elasticity 1993;31(3):189–208.

- Green AE, Naghdi PM. On undamped heat waves in an elastic solid. J Thermal Stresses 1992;15(2):253–64.

- Tzou DY. A unified field approach for heat conduction from macro- to micro-scales. J Heat Transfer 1995;117(1):8–16.

- Cattaneo C. Sur une forme de l’équation de la chaleur… C R Acad Sci 1958;247:431–3.

- Vernotte P. Les paradoxes de la théorie continue de l’équation de la chaleur. C R Acad Sci 1958;246:3154–5.

- Bagri A, Eslami MR. A unified generalized thermoelasticity; solution for cylinders and spheres. Int J Mech Sci 2007;49(12):1325–35.

- Ignaczak J, Ostoja-Starzewski M. Thermoelasticity with Finite Wave Speeds. Oxford University Press; 2010.

- Hosseini SM, Abolbashari MH. Analytical solution for thermoelastic waves propagation in functionally graded cylinders without energy dissipation. J Thermal Stresses 2012.

- Heydarpour Y, et al. Thermoelastic analysis of FG-GPLRC spherical shells based on Lord–Shulman theory. Compos Part B 2019;164:400–24.

- Hosseini SM. Thermal shock response of graphene/CNT-reinforced structures under Gaussian heat source. Thin-Walled Struct 2021;166:108108.

- Sherief HH, Elmisiery AEM, Elhagary MA. Generalized thermoelastic problem for an infinitely long hollow cylinder for short times. J Thermal Stresses 2004;27(10).

- [Paper 1 of this series — cite as submitted / in press.]

## Submission checklist

- Confirm the GN-III boundary-condition approximation is stated explicitly (documented in the thesis as an approximation — a referee will look for it)

- State the parametric status of the large τ₀ values up front, not in response to review

- Keep §3 short; the full formulation belongs to Paper 1 and must not be reproduced verbatim

- Verify no figure here is also used in Paper 1 (allocation is in the portfolio note)

- Author order and thesis footnote