# Chapter 5: Conclusions and Recommendations

## 5-1. Introduction

In this thesis, the transient thermoelastic behavior of a multilayer porous GPL-reinforced hollow cylinder under thermo-mechanical loading was solved in fully coupled form, based on the generalized Lord-Shulman theory, using the layerwise differential quadrature method in space and Newmark integration in time. The developed solver was verified through five independent tests and its convergence with respect to the number of layers and the spatial discretization was established; an extensive set of parametric studies and three extension studies were then carried out. This chapter summarizes the main findings, the contributions, and the recommendations for future work.

## 5-2. Main findings

- Thermal wave and temperature overshoot. Unlike classical Fourier conduction, in which the mid-wall temperature never exceeds the driving value, the Lord-Shulman theory permits a temperature overshoot (above unity) because of its finite wave-propagation speed. In the reference case the peak mid-wall temperature is 0.926 and does not exceed unity, but a genuine overshoot appears in cases such as porosity pattern V (1.109) and a high GPL weight fraction (up to 1.115). The temperature histories show the characteristic “peak-trough” shape produced by the wave travelling back and forth and reflecting from the outer surface, a phenomenon decisive in short-time analyses.

- GPL distribution pattern. Placing the conductive platelets at the heated inner surface (pattern V) gives the most favorable behavior, lowering the peak temperature by about 29 % relative to the uniform case and the inner-surface hoop stress by about 3 times. Pattern A is the mirror image of V and the worst case in all three quantities (temperature, stress and displacement).

- Porosity pattern and level. Porosity pattern A, concentrating the pores at the outer surface, acts as a “thermal barrier” and reduces the outer-surface temperature by about 8 times, but it also reverses the sign of the inner-surface hoop stress. Pattern V concentrates the pores at the inner surface and produces the largest transient peak of the group (1.11).

- Synergetic GPL-porosity interaction. Combining GPL-V (conductive facing the heat source) with porosity-A (insulating facing the environment) is synergetic and reduces the outer-surface temperature by about 26-fold at a benign stress level; this combination is the design recommendation of this work for thermal-protection applications. The complete 5×5 matrix showed that the mirror patterns V and A can be synergetic (GPL-V with porosity-A → 0.034) or cancelling (GPL-V with porosity-V → 0.692), so the alignment or opposition of the two patterns is decisive.

- Weight fraction and percolation threshold. A percolation threshold near a 1 % weight fraction switches the wall from a “thermal insulator” to a “thermal conductor”; adding graphene beyond that improves the thermal penetration only smoothly but mainly raises the thermal stresses (the stress doubles at 8 %).

- Platelet aspect ratios. The two ratios behave quite differently. The length-to-width ratio acts monotonically but saturates: raising it from 1 to 10 lifts the peak mid-point temperature only from 0.898 to 0.951, most of that in the first step, so that from a ratio of 4 upward the curves practically coincide. The width-to-thickness ratio, by contrast, is a threshold lever rather than a weak one: the conducting platelet network forms only once the volume fraction exceeds the inverse of the length-to-thickness ratio, which at the reference weight fraction means a width-to-thickness ratio above about 177. Below that threshold the effective conductivity falls back to that of the graphene-free porous matrix and the thermal wave does not reach mid-wall within the time window of the problem. The stiffness, however, still varies continuously with the same ratio, so two sub-threshold cases separate mechanically even though their temperature fields are identical.

- Coupling of the equations. The fully coupled solution damps the thermal wave by about 1 % (thermoelastic damping); uncoupled models are non-conservative exactly at the wave fronts.

- Internal pressure and supports. The internal pressure is a second-order effect at small engineering magnitude, but in the 70–100 MPa range it becomes a genuine secondary effect (up to about 50 % of the inner hoop stress); the response nonetheless remains thermally dominated and, in the present linear model, no discontinuity occurs up to 100 MPa. Clamped supports, by blocking axial expansion, reduce the peak mid-length radial displacement by about 9 %; support effects are localized at the ends, and as the cylinder lengthens the mid-length response converges to the infinite-length limit.

- Impulsive thermal shock. Under a Gaussian pulse, the classical theory underestimates the peak temperature by about 2.5 times — one of the strongest arguments of this work in favor of the generalized theory.

- Methodological findings. Newmark offers the best accuracy-to-cost ratio of the six tested integrators; differential quadrature needs about 15 times fewer points per direction than finite differences or linear finite elements; and the four-theory map (Fourier / Lord-Shulman / DPL / Green-Naghdi) charts where the theories diverge (the DPL degeneracy at τT=τq and the persistent Green-Naghdi overshoot).

## 5-3. Contributions

- A fully coupled Lord-Shulman thermoelastic solution for the multilayer porous GPL-reinforced cylinder by a two-dimensional (r,z) layerwise differential quadrature method.

- Identification of the synergetic interaction of the GPL-V and porosity-A patterns and presentation of the complete 5×5 interaction matrix, which has no counterpart in previous references.

- Reporting the “peak-trough” and mirror behavior of the patterns and linking it to the wave-like nature of the conduction.

- Three methodological extension studies: a comparison of six time integrators, four spatial discretizations (including linear/quadratic Galerkin finite elements) and four thermoelasticity theories with matched parameters.

## 5-4. Limitations of the study

As with any numerical study, this work was carried out within a specific set of assumptions and boundaries that should be kept in mind when interpreting or generalizing the results:

- Linear elastic model, no damage/failure criterion. Stresses and displacements throughout this work — including under large loads such as a 100 MPa internal pressure or an impulsive thermal shock — are reported under the linear-elasticity assumption. The model has no yield, cracking, or interlayer-separation criterion; under very large loads, the results should therefore be read as the mathematical extrapolation of a linear model, not a prediction of actual material failure.

- Temperature-independent material properties. Young’s modulus, thermal conductivity, the thermal expansion coefficient, and specific heat are held constant throughout the solution, while the reference loading takes the inner-surface temperature from 300 to 600 K; over this range, the real temperature-dependence of the material properties is not negligible.

- Isotropic homogenization of the composite layer. The elastic matrix of the GPL-matrix layer is reduced to a single effective isotropic modulus via the Halpin-Tsai average (Es=38EL+58ET); a real nanocomposite sheet is inherently transversely isotropic, and this simplification can shift the axial response somewhat.

- Ideal layer-to-layer bonding. Interfaces between layers enforce full continuity of temperature, flux, displacement, and traction; the thermal and mechanical contact resistance that is always present in a real layered structure is not included in the model.

- Qualitative validation of the wave-propagation core. The central claim of this work — the second-sound wave overshoot — is validated only qualitatively (matching the trend of speed and reflection) against the Bagri and Eslami results; no quantitative error metric is reported for this specific test.

- Selected porosity patterns. The porosity patterns used (UD, O, X, V, A) were chosen based on the standard open-cell metal-foam model; this is a deliberate modeling choice, not a complete representation of every possible porous microstructure.

- Geometric and loading scope. The study is limited to a straight cylindrical shell with simple/clamped/mixed supports and axisymmetric thermo-mechanical loading; conical or rotating geometries, non-axisymmetric loading, and fully three-dimensional effects lie outside the scope of this work.

## 5-5. Recommendations for future work

- Free/roller (F/R) supports: a stable implementation of these supports and the addition of a true plane-strain reference for a direct comparison with the infinite-length limit.

- Vectorized assembly: rewriting the assembly loop in vectorized form to reduce the computation time for larger grids and broader parametric studies.

- Temperature-dependent material properties: including the dependence of the modulus, conductivity and expansion coefficient on temperature, which is significant over the 300–600 K range.

- Radiation boundary condition: adding nonlinear radiative heat exchange at the outer surface for high-temperature applications.

- Damage/failure model: since the present linear thermoelastic model shows no discontinuity even at 100 MPa, adding a damage or failure model is necessary to predict rupture (material failure/separation) under very high loads.

- Updated porosity patterns: replacing the porosity patterns with the new patterns of the reference file and re-running the porosity and interaction studies.

- Geometric and loading extensions: functionally graded continuous distributions, other platelet geometries, a rotating cylinder, and three-dimensional effects.

- Experimental validation: fabricating physical specimens of the multilayer porous GPL-reinforced cylinder and testing them under a real thermal shock (e.g. laser or induction heating) to directly measure the second-sound overshoot and quantitatively validate the model; also an experimental measurement of the relaxation time τ0 for this specific material combination (via laser-flash or DSC methods), which is currently only a theoretical parameter.

- Applied design guidance: translating this work’s design finding (the GPL-V / porosity-A synergy) into a simple engineering selection chart or table for designers of thermal-protection layers (e.g. nuclear-reactor liners, hypersonic thermal-protection panels, industrial heat exchangers), without needing to run the full solver for every case; and a case study on standard industrial geometries (e.g. ASME dimensions) to give directly usable numbers beyond the dimensionless reference case.